## Slide 1: PRISMS Center Center for PRedictive Integrated Structural Materials Science
John C. Thomas, Brian Puchala, Anton Van der Ven Anirudh Natarajan, John Goiri, Min-Hua Chen, Max Radin, Jonathon Bechtel, Elizabeth Decolvenaere
PRISMS Center Workshop
August 15-17, 2016
Website: prisms-center.org
CASM Demo – Day 1

## Slide 2: A persisting problem
Source: http://www.lbl.gov/cs/html/exascale4energy

## Slide 3: A persisting problem
Source: http://www.lbl.gov/cs/html/exascale4energy

## Slide 4: From atoms to microns
Calculate accurate energies of the system in 102-103 different states

## Slide 5: From atoms to microns
Calculate accurate energies of the system in 102-103 different states
Solve
better than ~10 meV/atom
Chemical species
Charge states
Atomic displacement
Strain

## Slide 6: From atom- to micron-scale
Calculate accurate energies of the system in 102-103 different states
Identify suitable variables and basis functions for parameterizing energy model

## Slide 7: From atom- to micron-scale
Calculate accurate energies of the system in 102-103 different states
Identify suitable variables and basis functions for parameterizing energy model
Must be invariant to symmetry!!
Unknown

## Slide 8: From atom- to micron-scale
Calculate accurate energies of the system in 102-103 different states
Use model for material optimization or to simulate material properties
Identify suitable variables and basis functions for parameterizing energy model

## Slide 9: From atom- to micron-scale
Calculate accurate energies of the system in 102-103 different states
Use model for material optimization or to simulate material properties
Identify suitable variables and basis functions for parameterizing energy model
Free energy
Phase diagrams
Elastic tensors
Thermal conductivity
Diffusivity
Vibrational spectra
As a function of temperature, stress, chemical potential, etc.

## Slide 10: From atom- to micron-scale
Use model for material optimization or to simulate material properties
Identify suitable variables and basis functions for parameterizing energy model
Calculate accurate energies of the system in 102-103 different states
Share data with colleagues for experimental design or simulation at longer length/time scales

## Slide 11: From atom- to micron-scale
Use model for material optimization or to simulate material properties
Identify suitable variables and basis functions for parameterizing energy model
Calculate accurate energies of the system in 102-103 different states
Construct structural hypotheses of what happens in the real material
Share data with colleagues for experimental design or simulation at longer length/time scales

## Slide 12: From atom- to micron-scale
Use model for material optimization or to simulate material properties
Identify suitable variables and basis functions for parameterizing energy model
Calculate accurate energies of the system in 102-103 different states
Construct structural hypotheses of what happens in the real material
Share data with colleagues for experimental design or simulation at longer length/time scales

## Slide 13: CASM Tutorial Outline
Today:
Crystal structure identification & specification
Symmetry analysis
Using CASM to manage data
  Configuration selections and query syntax
  Maintaining sanity with cluster expansion profiles
Cluster expansion basics
  Configuration enumeration
  Cluster expansion basis sets & correlation evaluation
Tomorrow (with Brian Puchala):
Parameterizing cluster expansions
Predicting thermodynamic properties with grand canonical Monte Carlo
Free energy integration and phase diagram construction

## Slide 14: CASM: Clusters Approach to Statistical Mechanics
First-principles energies of a “few” excitations
Lattice Model Hamiltonian
Monte Carlo
Thermodynamics
Extrapolate to
all other excitations

## Slide 15: Lithium ion batteries
LixCoO2 LixTiS2 Li(Ni0.5Mn0.5)O2
Li
LixM

## Slide 16: Electrochemical measurements and thermodynamics
Li
LixM
Gibbs free energy

## Slide 17: Electrochemical measurements and thermodynamics

## Slide 18: Electrochemical measurements and thermodynamics

## Slide 19: Layered LixTiS2

## Slide 20: Configurational degrees of freedom
Lithium-vacancy disorder over interstitial sites

## Slide 21: Configurational degrees of freedom
Lithium-vacancy disorder over interstitial sites
Total of 2N configurations

## Slide 22: Density Functional Theory
Energy
Lattice parameters
Charge density
Generalized Gradient (GGA)
Approximation
Local density (LDA)
= charge density

## Slide 23: Layered LiTiS2
DFT (LDA), PAW method using VASP
Formation energies at zero Kelvin

## Slide 24: Tutorial Project: Zr-O binary system
Zr:
  Very high O solubility
ZrOx
  Series of suboxide phases
ZrO2-x
  Oxide
J.P. Abriata, J. Garcés, and R. Versaci, Bulletin of Alloy Phase Diagrams Vol. 7 No. 2 1986 .

## Slide 25: Nature of ZrO1/2 disordering transitions?
“the rearrangement of the oxygen atoms from uneven to even distribution on the neighboring interstice planes, and then [to a] random distribution in each plane.” or is low temperature transition first order?
Arai and Hirabayashi, J. Less-Common Metals, 44, 291 (1976).
Burton, Van de Walle, and Stokes, J. Phys. Soc. Japan, 81, 014004 (2012).

## Slide 26
v0.2.0 Now Available!

## Slide 27: CASM Design Principles
Log all commands over the course of a project
Try to record provenance of all data as part of normal workflow
Reproducibility
Tools to generate, screen, and dispatch DFT calculations, and then organize, filter, and analyze the results.
Managed directory tree and dependency framework that allows multiple calculation and model parameters to be tested and compared within a single project
Data Management and Automation
Most input and output files are stored in JavaScript Object Notation (JSON)file formats, which is widely used and highly readable.
Weak coupling between CASM and DFT codes, so that CASM can be adapted to work with various existing and future codes.
Interoperability

## Slide 28: CASM Design Principles
Collaboration
Efficiency
Easy archival of projects (‘casm files’ command), with granular control over amount and type of data to include.
Parameterized physics models can be shared without data and used to perform finite-temperature simulation
CASM implements unique and highly optimized algorithms for generating and analyzing data and building physics models.
Models are automatically converted to optimized C++ code and then compiled for use in Monte Carlo, enabling larger simulations and improved convergence.

## Slide 29: CASM: Overview
Specify the problem: a crystal in which one or more sites has multiple possible occupants:
  Oct (O) in HCP-based ZrOx
  Ni—Al substitution in FCC NixAl1-x
Enumerate many possible symmetrically distinct configurations of the crystal and for each one (i)
  Calculate energy E(i)
  Calculate symmetry-invariant correlation vector (the configuration’s “fingerprint”)
Fit the linear functional that is the best approximation of E(i)
Use to run Monte Carlo simulations and calculate finite-temperature properties

## Slide 30: Problem Definition

## Slide 31: Problem Definition

## Slide 32: Problem Definition
a
b
Lattice Vectors
x
y

## Slide 33: Problem Definition
Basis Atoms
a
b
Lattice Vectors
x
y

## Slide 34: Problem Definition
Lattice Vectors
Basis Atoms
a
b
{
"title" : "ZrO”,
"coordinate_mode" : "Fractional",
"description" : “HCP Zr with oct (O) ",
"lattice_vectors" : [
[ 3.233986860000, 0.000000000000, 0.000000000000 ],
[ -1.616993430000, 2.800714770000, 0.000000000000 ],
[ -0.000000000000, 0.000000000000, 5.168678340000 ]
],
"basis" : [
{
"coordinate" : [ 0.0000000, 0.0000000, 0.000000 ],
"occupant_dof" : [ "Zr" ]
},
{
"coordinate" : [ 0.6666667, 0.3333334, 0.500000 ],
"occupant_dof" : [ "Zr" ]
},
{
"coordinate" : [ 0.3333333, 0.6666667, 0.250000 ],
"occupant_dof" : [ "Va", "O" ]
},
{
"coordinate" : [ 0.3333333, 0.6666667, 0.750000 ],
"occupant_dof" : [ "Va", "O" ]
}
]
}
prim.json:
x
y

## Slide 35: Problem Definition
Lattice Vectors
Basis Atoms
a
b
{
"title" : "ZrO”,
"coordinate_mode" : "Fractional",
"description" : “HCP Zr with oct (O) ",
"lattice_vectors" : [
[ 3.233986860000, 0.000000000000, 0.000000000000 ],
[ -1.616993430000, 2.800714770000, 0.000000000000 ],
[ -0.000000000000, 0.000000000000, 5.168678340000 ]
],
"basis" : [
{
"coordinate" : [ 0.0000000, 0.0000000, 0.000000 ],
"occupant_dof" : [ "Zr" ]
},
{
"coordinate" : [ 0.6666667, 0.3333334, 0.500000 ],
"occupant_dof" : [ "Zr" ]
},
{
"coordinate" : [ 0.3333333, 0.6666667, 0.250000 ],
"occupant_dof" : [ "Va", "O" ]
},
{
"coordinate" : [ 0.3333333, 0.6666667, 0.750000 ],
"occupant_dof" : [ "Va", "O" ]
}
]
}
prim.json:
a
b
c
x
y
x
y
z

## Slide 36: Problem Definition
Lattice Vectors
Basis Atoms
a
b
{
"title" : "ZrO”,
"coordinate_mode" : "Fractional",
"description" : “HCP Zr with oct (O) ",
"lattice_vectors" : [
[ 3.233986860000, 0.000000000000, 0.000000000000 ],
[ -1.616993430000, 2.800714770000, 0.000000000000 ],
[ -0.000000000000, 0.000000000000, 5.168678340000 ]
],
"basis" : [
{
"coordinate" : [ 0.0000000, 0.0000000, 0.000000 ],
"occupant_dof" : [ "Zr" ]
},
{
"coordinate" : [ 0.6666667, 0.3333334, 0.500000 ],
"occupant_dof" : [ "Zr" ]
},
{
"coordinate" : [ 0.3333333, 0.6666667, 0.250000 ],
"occupant_dof" : [ "Va", "O" ]
},
{
"coordinate" : [ 0.3333333, 0.6666667, 0.750000 ],
"occupant_dof" : [ "Va", "O" ]
}
]
}
prim.json:
a
b
c
x
y
x
y
z

## Slide 37: Problem Definition
Lattice Vectors
Basis Atoms
a
b
{
"title" : "ZrO”,
"coordinate_mode" : "Fractional",
"description" : “HCP Zr with oct (O) ",
"lattice_vectors" : [
[ 3.233986860000, 0.000000000000, 0.000000000000 ],
[ -1.616993430000, 2.800714770000, 0.000000000000 ],
[ -0.000000000000, 0.000000000000, 5.168678340000 ]
],
"basis" : [
{
"coordinate" : [ 0.0000000, 0.0000000, 0.000000 ],
"occupant_dof" : [ "Zr" ]
},
{
"coordinate" : [ 0.6666667, 0.3333334, 0.500000 ],
"occupant_dof" : [ "Zr" ]
},
{
"coordinate" : [ 0.3333333, 0.6666667, 0.250000 ],
"occupant_dof" : [ "Va", "O" ]
},
{
"coordinate" : [ 0.3333333, 0.6666667, 0.750000 ],
"occupant_dof" : [ "Va", "O" ]
}
]
}
prim.json:
a
b
c
JSON: JavaScript Object Notation
x
y
x
y
z

## Slide 38: Problem Definition
Lattice Vectors
Basis Atoms
a
b
// HCP Zr-O
1.00000000
1.61699343 2.80071477 0.00000000
-1.61699343 2.80071477 0.00000000
0.00000000 0.00000000 5.16867834
2 2
Direct
0.0000000 0.0000000 0.0000000 Zr
0.6666667 0.6666667 0.5000000 Zr
0.3333333 0.3333333 0.2500000 Va O
0.3333333 0.3333333 0.7500000 Va O
PRIM (legacy format):
a
b
c
Similar format to VASP POSCAR
x
y

## Slide 39: CASM: Getting started
Material
definition
Initialization
Generated
directories

## Slide 40: CASM: Getting started
Install 'casm' command line programs
'casm status'
  Quick look at your current project
  Suggestions for next steps
'casm format'
  Documentation of project directory and file formats
'casm –h'
  Help menus show allowed options

## Slide 41: Crystal Symmetry
Apply rotation, reflection, inversion, and/or rotation to the crystal.

## Slide 42: Crystal Symmetry
Apply rotation, reflection, inversion, and/or rotation to the crystal.
60°

## Slide 43: Crystal Symmetry
Apply rotation, reflection, inversion, and/or rotation to the crystal.
If the result is indistinguishable from the initial state, then that operation is in the crystal’s space group.
60°

## Slide 44: Crystal Symmetry
Common notation: {Rα|τ}
  Rα: point group operations such as rotations, reflections, improper rotations, inversions
  τ: translation vector
  α: 3x3 transformation matrix
M.S. Dresselhaus, G. Dresselhaus, and A. Jorio.
Group Theory: Application to the Physics of Condensed Matter.

## Slide 45: Symmetry
Lattice point group:
  Symmetry operations that map lattice onto itself, leaving origin invariant (rotation, mirror, inversion, rotoinversion)
Crystal factor group:
  Symmetry operations that map lattice and identical basis sites onto themselves (translations may result in screw axes or glide planes)
Crystal point group:
  Crystal factor group operations, with translations removed

## Slide 46: Crystal Configurations

## Slide 47: Crystal Configurations

## Slide 48: Crystal Configurations
Vol 2 Supercell
Vol 4 Supercell

## Slide 49: Crystal Configurations

## Slide 50: Crystal Configurations
60°
Equivalent!!

## Slide 51: Supercell Enumeration
Represent lattice using column vector matrices:
P: primitive lattice
S: supercell lattice
T: integer supercell transformation matrix
S1
S2
P1
P2
S1
S2
S1=P1 S2=2P2
S1=P1+P2 S2=-P1+P2

## Slide 52: Supercell Enumeration
Equivalent supercells:
Linear combination of supercell lattice vectors
S
S'

## Slide 53: Supercell Enumeration
Equivalent supercells:
Linear combination of symmetrically equivalent supercell lattice vectors
For a crystal, allowed symmetry operations depends on crystal basis
S
S'

## Slide 54: Supercell enumeration
If unit cell lattice, P, is represented as column vector matrix, then supercell lattices, S, are:
T is an integer supercell transformation matrix, and S has integer volume det(T), relative to the primitive cell.
Supercells are equivalent if for some T:
At a given volume (det(T)), loop over possible T matrices and use crystal point group operations to check if we've found a new symmetrically distinct supercell

## Slide 55: Supercell enumeration
SCEL4_1_4_1_0_0_0
Volume
Shape Factors
Max an min supercell volume can be specified for enumeration
Supercell enumeration can be restricted to 1D and 2D. See casm enum --help
for details.

## Slide 56: Configuration enumeration
A:
B:
Equivalent configurations:
Supercells of the volume 1 configuration

## Slide 57: Configuration enumeration
Equivalent configurations:
Translation maps one configuration onto the other
A:
B:

## Slide 58: Configuration enumeration
Equivalent configurations:
Rotation or translation maps occupants
A:
B:

## Slide 59: Configuration enumeration
Enumerate symmetrically unique configurations by:
  Loop over possible occupations
  Check all factor group operations that keep the supercell lattice vectors unchanged, in combination with all primitive cell translations within the supercell
  If translation within the supercell alone maps all occupants, then it is a supercell of a smaller primitive configuration

## Slide 60: Configuration enumeration
Configurations are enumerated ONLY in supercells that have been enumerated.
You can specify the min and max supercell volumes, or specify a supercell explicitly.
CAUTION: The number of unique configurations that fit in a supercell grows exponentially with supercell volume.

## Slide 61: Configuration visualization
Set up environment:
casm settings --set-view-command 'casm.view VESTA’
Try with one or more configuration names:
casm view SCEL4_2_2_1_0_0_1/25

## Slide 62: CASM Composition metrics
Each configuration has a composition, and there are various ways to measure it:
atom_frac: atom_frac(Au), atom_frac(Cu), etc.
  Number of Au, Cu, etc., divided by total number of atoms. Vacancies are ignored.
comp_n: comp_n(Au), comp_n(Cu), etc.
  Number of Au, Cu, etc., divided by number of primitive cells (volume). Accounts for vacancies.
comp: comp(a), comp(b), etc.
  Primitive-cell-based formula parameters (e.g., AuaCubPt(1-a-b)), determined by user-specified composition axes. Accounts for vacancies.
When vacancies are present, ‘atom_frac’ is qualitatively different from ‘comp_n’ and ‘comp’

## Slide 63: Specifying composition axes
Binary Compound:

## Slide 64: Specifying composition axes
Au
Pt
Cu
Cu1-a-bAubPta
CubAuaPt1-a-b
a
b
a
b
Ternary Compound:
Binary Compound:

## Slide 65: Specifying composition axes
Zr2O2a[Va]2(1-a)
Zr2O2(1-a)[Va]2a
NOTE: prim.json determines formula unit (2 Zr)

## Slide 66: Data Management
Project data is managed according to the parameters, settings, and timeline that it depends on:
  ‘calctype’ DFT parameters and setting (XC functional, pseudopotential, convergence parameters, etc.)
  ‘property’ The particular quantity being measured (formation_energy, volume_relaxation, etc.)
  ‘ref’ Baseline reference used for measuring quantity (zero-point of energy, reference volume, etc.)
  ‘bset’ Basis functions used to “fingerprint” configurations and in terms of which the property model is expressed .
  ‘eci’ The model parameters (effective cluster interactions) used to predict a particular property in terms of a particular basis set.
Manage and create settings profiles from the ‘casm settings’ command. A ‘default’ profile is created during project initialized.
Ex:
  DFT-calculated properties: Depend on ‘calctype’, ‘property’, and sometimes ‘ref’
  Cluster expansion/physics model: Depends on ‘calctype’, ‘property’, ‘ref’, ‘bset’
  Predicted properties and Monte Carlo Data: Depend on ‘calctype’, ‘property’, ‘ref’, ‘bset’, and ‘eci’

## Slide 67: Data Management Workflow
Info/Analysis
Configuration Database
Records configurations that have been enumerated or imported to a project and their associated data
Configuration Selection
References to subset of the configuration database.
CASM
Configuration Selection
Job Dispatch

## Slide 68: Working with selections
CASM query syntax provides simple interface to explore, screen, and select configurations.
Example:
casm select --set "eq(scel_size, 4)"
will select all configurations the belong to supercells of volume 4 (relative to primitive cell)
Many configuration properties are supported
  ‘scel_size’ Integer volume of supercell that contains the configuration
  ‘comp(a)’, ‘comp(b)’, etc. The chemical composition, in terms of composition axes
  ‘atom_frac(Au)’, etc. The atomic fraction of a particular specie
  ‘is_calculated’ True if DFT data exists for the configuration
  ‘formation_energy’ DFT formation energy (if calculated)
  ‘volume relaxation Change in volume due to relaxation (expressed as V/V0)
… and many others (for full listing see casm select --help properties)
Properties can be related and compared via operators
  arithmetic add, subtract, multiply, divide, sqrt, exp
  comparison equality, less-than, greater-than, etc.
  logical AND, OR, NOT, etc.
  ranges min, max, and others
  text search and match with regular expressions
for documentation see casm select --help operators

## Slide 69: Working with selections
Selections can be edited and combined using ‘casm select’
The ‘MASTER’ selection is stored in the configuration database and is the default selection for most operations. A selection can be redirected to a file using --output <filename>
Selection(s) to be operated can be read from a file using --configs <filename>
Edit selections using CASM query syntax
casm select --set <query> Create a selection from scratch
casm select --set-on <query> Set ‘selected’ from false to true if <query> is true
casm select --set-off <query> Set ‘selected’ from true to false if <query> is true
Combine selections using logical operators (AND, OR, NOT, XOR)

## Slide 70: Working with selections
Selections can be edited and combined using ‘casm select’
The ‘MASTER’ selection is stored in the configuration database and is the default selection for most operations. A selection can be redirected to a file using --output <filename>
Selection(s) to be operated can be read from a file using --configs <filename>
Edit selections using CASM query syntax
casm select --set <query> Create a selection from scratch
casm select --set-on <query> Set ‘selected’ from false to true if <query> is true
casm select --set-off <query> Set ‘selected’ from true to false if <query> is true
Combine selections using logical operators (AND, OR, NOT, XOR)
Predefined selections:
‘ALL’: specifies the total configuration database.
‘CALCULATED’: specifies all configurations for which DFT data exist.
‘NONE’: equivalent to ‘ALL’ but with all ‘selected’ bits set to 0

## Slide 71: CASM Query Syntax, Part II
CASM query syntax provides simple interface to explore, screen, and select configurations.
Use ‘casm query’ to print properties of selected configurations (supports JSON and CSV)
Example:
casm query --columns "comp(a)" "formation_energy" --configs select.csv
will print ‘casm select’-style CSV output to the screen:
output can be redirected to a file with --output <filename>
Query syntax can also be used to screen configurations at the enumeration stage, so they don’t pollute the configuration database.
Example:
casm enum --configurations --all --filter "lt(atom_frac(O),0.25)"
will only enumerate configurations that are dilute in oxygen (having O atomic fraction less than 0.25)

## Slide 72: DFT calculations
Provide DFT code input files and parameters
  Pseudopotentials, k-point density, energy cut-off, and settings files
Use ‘casm select’ to identify a selection of configurations to calculate
casm run –e vasp.relax --configs my_selection.csv
  vasp.relax is python script that automates job submission for each configuration. It submits the DFT calculation, handles common errors, ensures that results are converged and relaxed, and writes results to a format CASM understands (properties.calc.json).
  Uses ‘pbs’ python module to automate job submission (https://github.com/prisms-center/pbs)
Current support for VASP, support for other codes is planned. Contributions from the user community are encouraged!

## Slide 73: properties.calc.json files
CASM interprets calculation data from properties.calc.json file
Generated by ‘vasp.relax’ or manually using ‘vasp.relax.report’
$ROOT/training_data/$SCEL/$CONFIGID/calctype.$CALCTYPE/

## Slide 74: Relaxations and Mapping/Import
casm update:
  Read all new property files, and check relaxation
lattice_deformation (LD):
  Degree of homogeneous strain (per atom)
basis_deformation (BD):
  Mean square displacement
total deformation cost:
  w*LD+(1-w)*BD , 0<w<1
casm import:
  Use same algorithms as casm update to add ideal or relaxed configurations to project (even if not enumerated)
Very large relaxations may change the configuration. Conflicts can be resolved using either min-energy or min-deformation rule

## Slide 75: Setting energy reference
Chemical energy can only be measured relative to reference compounds

## Slide 76: Setting energy reference
Chemical energy can only be measured relative to reference compounds

## Slide 77: Setting energy reference
Chemical energy can only be measured relative to reference compounds
casm ref --set-auto will attempt to set energy references as near to extreme stoichiometries as possible (left case)

## Slide 78: CASM: Clusters Approach to Statistical Mechanics
First-principles energies of a “few” excitations
Lattice Model Hamiltonian
Monte Carlo
Thermodynamics
Extrapolate to
all other excitations

## Slide 79: Zr-O system
Puchala and Van der Ven, Phys. Rev. B 88 094108 (2013).
Each red circle specifies belongs to a specific configuration of HCP-based ZrOx

## Slide 80: Zr-O system
ZrO1/3
ZrO1/2
ZrO1/6
Puchala and Van der Ven, Phys. Rev. B 88 094108 (2013).
A
BC
A
BC
A
BC
A
-
B
C
A
-
-
A
B
C
A
B
C

## Slide 81: Zr-O system
O stacking sequences
Puchala and Van der Ven, Phys. Rev. B 88 094108 (2013).
ZrO1/6-ZrO1/3
ZrO1/3-ZrO1/2
ZrO1/6 if X = 0
ZrO1/2 if X = 2/3
de Fontaine, Nature 343, 544 (1990).

## Slide 82: CASM: Clusters Approach to Statistical Mechanics
First-principles energies of a “few” excitations
Lattice Model Hamiltonian
Monte Carlo
Thermodynamics
Extrapolate to
all other excitations

## Slide 83: The Clusters Approach to Statistical Mechanics
Is there a compact way to approximate the energy of any configuration?
x
y

## Slide 84: The Clusters Approach to Statistical Mechanics
Species A
Species B
Is there a compact way to approximate the energy of any configuration?
x
y

## Slide 85: The Clusters Approach to Statistical Mechanics
Is there a compact way to approximate the energy of any configuration?
Species A
Species B
x
y

## Slide 86: The Clusters Approach to Statistical Mechanics
Is there a compact way to approximate the energy of any configuration?
Species A
Species B
x
y

## Slide 87: The Clusters Approach to Statistical Mechanics
Is there a compact way to approximate the energy of any configuration?
Species A
Species B
x
y

## Slide 88: The Clusters Approach to Statistical Mechanics
Is there a compact way to approximate the energy of any configuration?
Species A
Species B
x
y

## Slide 89: The Clusters Approach to Statistical Mechanics
Is there a compact way to approximate the energy of any configuration?
Species A
Species B
x
y

## Slide 90: The Clusters Approach to Statistical Mechanics
Species A
Species B
x
y
The orbit of the the NN pair
Is there a compact way to approximate the energy of any configuration?
Symmetric averages of measurements of cluster occupation states.

## Slide 91: The Clusters Approach to Statistical Mechanics
Species A
Species B
x
y
Is there a compact way to approximate the energy of any configuration?
Symmetric averages of measurements of cluster occupation states.

## Slide 92: The Clusters Approach to Statistical Mechanics
Is there a compact way to approximate the energy of any configuration?
Symmetric averages of measurements of cluster occupation states.
Species A
Species B
x
y

## Slide 93: The Cluster Expansion
Species A
Species B
x
y

## Slide 94: The Cluster Expansion
The occupant of lattice site i is described by the variable σi :
σi = +1 if species A
σi = -1 if species B
σ15
σ16
σ17
σ14
σ5
σ6
σ18
σ13
σ4
σ1
σ7
σ19
σ12
σ3
σ2
σ11
σ10
σ9
σ8
Species A
Species B

## Slide 95: The Cluster Expansion
Interactions between sites are described by products of σi .
Fit interaction parameters to a database of DFT energies.
Then use symmetry to average over the entire crystal
E = J11 + J1,717 + J1,18118 + J1,17117 + J1,4,5145 + . . .
σ15
σ16
σ17
σ14
σ5
σ6
σ18
σ13
σ4
σ1
σ7
σ19
σ12
σ3
σ2
σ11
σ10
σ9
σ8

## Slide 96: Cluster Expansion Example
σ15
σ16
σ17
σ14
σ5
σ6
σ18
σ13
σ4
σ1
σ7
σ19
σ12
σ3
σ2
σ11
σ10
σ9
σ8

## Slide 97: Cluster Expansion Example
σ15
σ16
σ17
σ14
σ5
σ6
σ18
σ13
σ4
σ1
σ7
σ19
σ12
σ3
σ2
σ11
σ10
σ9
σ8
Average site occupation is Γ1=(1 + 6)/2=0

## Slide 98: Cluster Expansion Example
σ15
σ16
σ17
σ14
σ5
σ6
σ18
σ13
σ4
σ1
σ7
σ19
σ12
σ3
σ2
σ11
σ10
σ9
σ8
Average site occupation is Γ1=(1 + 6)/2=0

## Slide 99: Cluster Expansion Example
σ15
σ16
σ17
σ14
σ5
σ6
σ18
σ13
σ4
σ1
σ7
σ19
σ12
σ3
σ2
σ11
σ10
σ9
σ8
Average site occupation is Γ1=(1 + 6)/2=0
Average NN pair occupation is Γ2=(17 + 16 + 15 + 618 + 617 + 616)/6 = 1/3

## Slide 100: Cluster Expansion Example
σ15
σ16
σ17
σ14
σ5
σ6
σ18
σ13
σ4
σ1
σ7
σ19
σ12
σ3
σ2
σ11
σ10
σ9
σ8
σ15
σ16
σ17
σ14
σ5
σ6
σ18
σ13
σ4
σ1
σ7
σ19
σ12
σ3
σ2
σ11
σ10
σ9
σ8
Correlations are identical for symmetrically equivalent configurations

## Slide 101: The bspecs.json file
Specifications for generating clusters and the cluster expansion basis functions

## Slide 102: The clust.json file
Lists one example (“prototype”) of each cluster type

## Slide 103: The clexulator (ZrO_Clexulator.cc)
Generated code for evaluating basis functions
Generated code for evaluating basis functions

## Slide 104: Cluster expansion for hcp Zr-O

## Slide 105: Cluster expansion for hcp Zr-O
Puchala and Van der Ven, Phys. Rev. B 88 094108 (2013).

## Slide 106: CASM: Clusters Approach to Statistical Mechanics
First-principles energies of a “few” excitations
Lattice Model Hamiltonian
Monte Carlo
Thermodynamics
Extrapolate to
all other excitations

## Slide 107: Summary
Crystal structure identification & specification
Symmetry analysis
Using CASM to manage data
  Configuration selections and query syntax
  Maintaining sanity with cluster expansion profiles
Cluster expansion basics
  Configuration enumeration
  Cluster expansion basis sets & correlation evaluation
Tomorrow (with Brian Puchala):
Parameterizing cluster expansions
Predicting thermodynamic properties with grand canonical Monte Carlo
Free energy integration and phase diagram construction