## Slide 1: PRISMS Center Center for PRedictive Integrated Structural Materials Science
Brian Puchala, John C. Thomas, Anton Van der Ven
Anirudh Natarajan, John Goiri, Min-Hua Chen, Max Radin, Jonathon Bechtel, Elizabeth Decolvenaere, Anna Belak,
Naga Sri Harsha Gunda, Sanjeev Kolli
TMS ICME 2017
Thurs. May 24, 2017
Website: prisms-center.org
CASM Tutorial – Section 2

## Slide 2: CASM Tutorial Outline
1:30 – 3:00:
Crystal structure identification & specification
Symmetry analysis
Using CASM to manage data
  Configuration selections and query syntax
  Maintaining sanity with cluster expansion profiles
Cluster expansion basics
  Configuration enumeration
  Cluster expansion basis sets & correlation evaluation
3:30 – 5:00:
Parameterizing cluster expansions
Predicting thermodynamic properties with grand canonical Monte Carlo
Free energy integration and phase diagram construction

## Slide 3: CASM: Clusters Approach to Statistical Mechanics
First-principles energies of a “few” excitations
Lattice Model Hamiltonian
Monte Carlo
Thermodynamics
Extrapolate to
all other excitations

## Slide 4: Zr-O binary system
Zr:
  Very high O solubility
ZrOx
  Series of suboxide phases
ZrO2-x
  Oxide
J.P. Abriata, J. Garcés, and R. Versaci, Bulletin of Alloy Phase Diagrams Vol. 7 No. 2 1986 .

## Slide 5: Query calculation results
'casm query -c CALCULATED -k 'comp formation_energy hull_dist(CALCULATED)'
  --output <filename> to output to file

## Slide 6: Plot calculation results, via Python
from casm.project import Project, Selection
import matplotlib.pyplot as plt
# construct a 'Selection'
proj = Project()
sel = Selection(proj, 'CALCULATED', all=False)
# query results into a pandas.DataFrame
comp = 'comp(a)'
Ef = 'formation_energy'
hull_dist = 'hull_dist(CALCULATED,atom_frac)'
sel.query([comp, Ef, hull_dist])
# get convex hull configurations,
# sorted for nice plotting
df = sel.data.sort_values([comp])
hull_tol = 1e-6
df_hull = df[df[hull_dist] < hull_tol]
print df_hull.to_string()
# plot formation energies with convex hull
plt.scatter(sel.data[comp], sel.data[Ef],
marker='o')
plt.plot(df_hull[comp], df_hull[Ef], 'b.-')
plt.xlabel(comp)
plt.ylabel('Formation energy (eV/unit cell)')
plt.xlim([0.,1.])
plt.show()

## Slide 7: The Cluster Expansion
Interactions between sites are described by products of σi .
Fit interaction parameters to a database of DFT energies.
Then use symmetry to average over the entire crystal
E = J11 + J1,717 + J1,18118 + J1,17117 + J1,4,5145 + . . .
σ15
σ16
σ17
σ14
σ5
σ6
σ18
σ13
σ4
σ1
σ7
σ19
σ12
σ3
σ2
σ11
σ10
σ9
σ8

## Slide 8: The bspecs.json file
Specifications for generating the cluster expansion basis functions

## Slide 9: Viewing cluster basis functions
'casm bset –functions' will print basis function formulas

## Slide 10: Query correlations
'casm query -k corr(0:5)'
  will print correlations, , the symmetry-invariant basis function averages
Next step: Fit cluster expansion paramters, , to the DFT calculated energies

## Slide 11: casm-learn
Acts as a wrapper around 'scikit-learn', the Python machine learning package, and incorporates some additional features:
  Genetic algorithms, via 'deap', the Distributed Evolutionary Algorithm Package
  Stores and compares potential results in a 'Hall Of Fame'
  Convex hull checking
  Generate casm selection files of configurations that you might want to calculate based on the cluster expansion
  Writes 'eci.json' file containing calculated parameters
scikit-learn: http://scikit-learn.org
deap: http://deap.readthedocs.io

## Slide 12: casm-learn: getting started
'casm-learn --help'
  Print available options
'casm-learn --desc'
  Print overall usage description
'casm-learn --exSomething'
  Print example input files
'casm-learn –settings-format'
  Print input file help
'casm-learn –s <filename>'
  Run, using <filename> as the input settings file

## Slide 13: Step 1) Problem specification
  Solve X*b = y for b
    X: 2d matrix of correlations
    y: 1d vector of formation energies (or other property)
    b: 1d vector, of fitting parameters, the effective clusters interactions (ECI)
  Weighted least squares
    X*b = y  L*X*b = L*y,
    W = L*LT, W typically being a diagonal matrix where the entries along the diagonal are the weights associated with each configuration

## Slide 14: Step 1) Problem specification
  Cross-validation:
    Seperate data into several training and testing sets
    For each training set, solve Xtrain*b = ytrain for b
    Use b to predict ytest = Xtest*b for the remaining data
    Calculate cross-validation score, root average MSE over test sets:
    'casm-learn' can optionally add an additional 'penalty', p, to prefer results with fewer terms

## Slide 15: Step 1) Problem specification
Cross-validation schemes:
  KFold cross validation: split data into 'k' "folds"
    Train the model on k-1 folds
    Test on the remaining fold
    CV score = Average score over each test fold
  LeaveOneOut: k = number of configurations
  ShuffleSplit:
    Create 'n_iter' random splits of the data, with user control of the fraction of configurations in the train/test sets
  Others:
  http://scikit-learn.org/stable/modules/cross_validation.html#cross-validation

## Slide 16: Step 1) Problem specification
scikit-learn class name and keyword arguments, as documented on scikit-learn.org
weighting method name and keyword arguments, as documented in
'casm-learn –settings-format'
optional penalty per non-zero eci, as documented in
'casm-learn –settings-format'
name of a 'casm select' output file, or "CALCULATED", or "MASTER",

## Slide 17: Step 2) Estimator and Feature Selection Methods
Estimator:
  determines how to solve for b, given X and y
  Examples: LinearRegression, Lasso, Ridge
  http://scikit-learn.org/stable/modules/linear_model.html
Feature Selection:
  Determines which features (basis functions) to include in the model (which subset of bi are non-zero)
  Examples: GeneticAlgorithm, RFE (recursive feature elimination), SelectFromModel (used with Lasso, for example)
  http://scikit-learn.org/stable/modules/feature_selection.html

## Slide 18: Step 2) Estimator and Feature Selection Methods
scikit-learn class name and keyword arguments, as documented on scikit-learn.org
scikit-learn class name or casm.learn.evolve class name and keyword arguments, as documented on scikit-learn.org and in 'casm-learn –settings-format'

## Slide 19: Step 2) Estimator and Feature Selection Methods
Run 'casm-learn': 'casm-learn -s fit_1.json'
  First time: stores problem specs in 'fit_1_specs.pkl'
  First time, and subsequent times: Runs and stores results in 'fit_1_halloffame.pkl'
For a single problem specification, you may run repeatedly with the same or different estimator and feature selection methods
  Individual results with best CV scores stored in hall of fame
View results: 'casm-learn -s fit_1.json --hall'
  '--format type', with type=details, json, csv
  '--indiv 0 1 ...', to only print particular individuals in the hall of fame

## Slide 20: Step 3 / 4) Analyze Results, Run Monte Carlo
'casm-learn -s fit_1.json --checkhull'
  Check if predicted ground state configurations agree with the DFT calculated ground state configurations
  Print configuration selection files with configurations that you may want to calculate
Compare results from different problem specs
  add more calculated configurations
  select different training configurations
  different weighting schemes
  different CV schemes
Compare Monte Carlo results
  'casm-learn –s fit.json –select 0' to write 'eci.json' file with ECI to use to evaluate the cluster expansion
  Run Monte Carlo calculations and check phase stability predictions

## Slide 21: The 'basis.json'/'eci.json' file
Contains descriptions of the site basis functions (not shown) and cluster basis functions
The 'basis.json' file is generated when using 'casm bset –update'
The 'eci.json' file is a copy of the 'basis.json' file with "eci": value added to cluster functions with non-zero eci.

## Slide 22: CASM: Clusters Approach to Statistical Mechanics
First-principles energies of a “few” excitations
Lattice Model Hamiltonian
Monte Carlo
Thermodynamics
Extrapolate to
all other excitations

## Slide 23: Composition conversions
: #atoms per unit cell
: #atoms per unit cell at composition axes origin
: formula parameters determined from user specified composition axes
: conversion matrix
: left pseudo-inverse

## Slide 24: Parametric chemical potential
Define:
: parametric chemical potential, along composition axes
- 'param_chem_pot' in casm input / output
: unit cell reference potential

## Slide 25: Example: Binary alloy, no Va
First choice of composition axes:

## Slide 26: Example: Binary alloy, no Va
Second choice of composition axes:

## Slide 27: Ternary Alloy

## Slide 28: Semi-grand canonical ensemble
By first & second laws, the fundamental equation is:
with a constraint on the total number of sites:

## Slide 29: Characteristic potential in semi-grand canonical ensemble
And partition function:

## Slide 30: Equations of state
Combining differentials of the fundamental equation and characteristic potential:

## Slide 31: Thermodynamic Integration
: potential energy per unit cell
: ensemble average
Free energy:
Partition function:

## Slide 32: Thermodynamic Integration
From the partition function and ensemble average:
From free energy:

## Slide 33: Thermodynamic Integration
From the partition function and ensemble average:
From free energy:

## Slide 34: Reference states
Low temperature expansion
  At low T, only the lowest energy configurations (ground state, and most stable perturbations) will contribute to the partition function. Evaluate partition function explicitly by enumerating 1, 2, ... occupant perturbations. CASM implements the approximation with only 1 occupant perturbations.

## Slide 35: Reference states
Dilute concentration:

## Slide 36: Importance sampling
To numerically average thermodynamic quantities,
you don't want to randomly sample from the 2N possibilities
Instead you want to sample configurations
with their probability of occurrence

## Slide 37: Monte Carlo Algorithm
A Monte Carlo Algorithm
    1. Start with some configuration
    2. Choose perturbation of the system
    3. Compute energy for that perturbation
    4. If accept perturbation
    If accept perturbation if a random number
5. Choose next perturbation
Property will be average over these states

## Slide 38: Monte Carlo output (Semi-grand Canonical)
Thermodynamic variables controlled in Monte Carlo (i.e. input)
Output from Monte Carlo

## Slide 39: Monte Carlo output (Semi-grand Canonical)

## Slide 40: Monte Carlo
See 'casm monte -h' and 'casm format --monte' for help setting up an input file.
The input file lets you specify:
  The cluster expansion
  Supercell and initial configuration
  Pathway in space, with dependent or independent runs
  Monte Carlo ensemble:
    "grand_canonical" (only option currently) for semi-grand canonical ensemble
  Monte Carlo method:
    'metropolis' or 'lte1' (low temperature expansion)
  Quantities to sample & convergence criteria
  Enable saving configurations encountered during Monte Carlo into your configuration list

## Slide 41: Monte Carlo Convergence
All quantities that are given a requested precision must first equilibrate, and then the estimated precision on the average must converge to the requested precision
  A. van de Walle, M. Asta, Modell. Simul. Mater. Sci. Eng. 10, 521 (2002)

## Slide 42: Phase diagram construction

## Slide 43: Phase diagram construction

## Slide 44: Phase diagram construction

## Slide 45: Phase diagram construction

## Slide 46: Phase diagram construction

## Slide 47: Calculated phase diagram
ZrO1/2
ZrO1/3
ZrO1/6
ZrO

## Slide 48: CASM Tutorial Outline
1:30 – 3:00:
Crystal structure identification & specification
Symmetry analysis
Using CASM to manage data
  Configuration selections and query syntax
  Maintaining sanity with cluster expansion profiles
Cluster expansion basics
  Configuration enumeration
  Cluster expansion basis sets & correlation evaluation
3:30 – 5:00:
Parameterizing cluster expansions
Predicting thermodynamic properties with grand canonical Monte Carlo
Free energy integration and phase diagram construction