## Slide 1: PRISMS Center Center for PRedictive Integrated Structural Materials Science
Brian Puchala, John C. Thomas, Anton Van der Ven
Anirudh Natarajan, John Goiri, Min-Hua Chen, Max Radin, Jonathon Bechtel, Elizabeth Decolvenaere, Anna Belak,
Naga Sri Harsha Gunda, Sanjeev Kolli
TMS ICME 2017
Thurs. May 24, 2017
Website: prisms-center.org
CASM Tutorial – Intro

## Slide 2
Phenomenological
descriptions
Electronic structure
Statistical Mechanics
Thermodynamics
Kinetics
Solid Mechanics
Linking atomistic descriptions to phenomenological models of materials
Notes: Many of the most important or useful descriptions of materials behaviour are continuum descriptions.
Phase stability, mechanical properties, and microstructure evolution, can all be understood in terms of the free energy and kinetic coefficients of particular materials.
But of course these quantities fundamentally depend on atomistic interactions.
Our work is focused on using methods of statistical mechanics to link accurate ab initio electronic structure calculations of atomistic systems to phenomenological descriptions of materials.

## Slide 3
Phenomenological
descriptions
Electronic structure
Via rigorous and arbitrarily extendible cluster expansion Hamiltonians
Statistical Mechanics
Cluster Expansion Hamiltonians
Q1
Notes: We do this by constructing cluster expansion effective Hamiltonians in terms of atomic degrees of freedom.
These descriptions are nearly as accurate as electronic structure calculations, but orders of magnitude faster, enabling monte carlo calculations of thermodynamic and kinetic quantities.
The methods we use have many applications, but today I'll just talk about how we've applied it to basic science of the thermodynamics in the Zr-O-H system.

## Slide 4: PRISMS Center Integrated Framework
Real Space DFT
(PRISMS-RSDFT)
Fourier Space DFT
(VASP)
Atomic scale
constitutive laws
Statistical Mechanics
(CASM)
Phase Diagrams
(CASM/CALPHAD)
Dislocation Dynamics
(LLNL-ParaDIS)
Phase Field Crystal
(PRISMS-PFC*)
Phase Field
(PRISMS-PF)
Crystal Plasticity
(PRISMS-Plasticity)
Continuum Plasticity
(PRISMS-Plasticity)
Experiments (slip,
twinning, crack, etc.)
Mechano-Chemistry
(PRISMS-MC*)
Experiments

## Slide 5: Using ICME to Investigate Mg-Nd β’’’ Composition and Morphology
Fourier Space DFT
(VASP)
Statistical Mechanics
(CASM)
Phase Field
(PRISMS-PF)
Experiments
(HAADF-STEM)
Precipitate Dimensions
(Validation)
Finite Temp. Energies
0K Energies
Elastic Constants, Transformation Strains
Enumerate Configurations
Inform problem space
Natarajan et al., Acta Mater. 2016
Natarajan and Van der Ven, Acta Mater. 2017

## Slide 6: Examples: Calculated phase diagrams
Ti-O binary
Ni-Al binary
Mg-Nd binary
Zr-O binary

## Slide 7: Examples: Vibrational excitations
Phonon Hamiltonian
M. H. Chen, B. Puchala, A. Van der Ven, CALPHAD (2015).
ZrO

## Slide 8: Examples: Calculated Zr-O phase diagram (configurational + vibrational excitations)
ZrO1/2
ZrO1/3
ZrO1/6
B. Puchala, A. Van der Ven, Physical Review B, 88, 094108 (2013).
ZrO2
ZrO
M. H. Chen, B. Puchala, A. Van der Ven, CALPHAD (2015).

## Slide 9: Examples: Anharmonic vibrational cluster expansion
J.C. Thomas and A. Van der Ven, Phys. Rev. B 88, 214111, (2013).
J.C. Thomas and A. Van der Ven, Phys. Rev. B 90, 214105, (2014)
Stress-free Monte Carlo simulations
Energy surface with homogeneous deviotoric deformation from DFT
Cubic–tetragonal phase transition in ZrH2
Stress free Monte Carlo
calculation

## Slide 10: Examples: Chemo-mechanical free energy
S. Rudraraju, A. Van der Ven & K. Garikipati, npj Computational Materials 2, 16012 (2016)

## Slide 11
Examples: Molecular occupation
JS Bechtel, R Seshadri, A. Van der Ven, J. Phys. Chem. C, 120, 12403 (2016)
Hybrid organic-inorganic ABX3 perovskites: CH3NH3PBI3

## Slide 12
Examples: Molecular occupation
JS Bechtel, R Seshadri, A. Van der Ven, J. Phys. Chem. C, 120, 12403 (2016)

## Slide 13: CASM Workflow
Problem specification
  Primitive crystal structure and allowed degrees of freedom
Enumerate configurations
Electronic structure calculations:
  Specify calculation parameters
Effective Hamiltonian specification:
  Specify cluster expansion basis set
Fit coefficients
Evaluate effective Hamiltonian:
  Monte Carlo calculation of ensemble averages
  Evaluate strain polynomials
Fit phenomenological models
  Free energy, mobilities
  For analysis and as input to models at greater time/length scales

## Slide 14: CASM Design Principles
Log all commands over the course of a project
Try to record provenance of all data as part of normal workflow
Reproducibility
Tools to generate, screen, and dispatch DFT calculations, and then organize, filter, and analyze the results.
Managed directory tree and dependency framework that allows multiple calculation and model parameters to be tested and compared within a single project
Data Management and Automation
CASM provides a set of tools and enables customization at many steps
As much as possible, CASM does not force you to use a particular method for enumeration, calculation, model fitting, etc.
Flexibility

## Slide 15: CASM Design Principles
Collaboration
Efficiency
Easy archival of projects (‘casm files’ command), with granular control over amount and type of data to include.
Parameterized physics models can be shared without DFT training data and used to perform finite-temperature calculations
CASM implements unique and highly optimized algorithms for generating and analyzing data and building physics models.
CASM generates optimized C++ code to evaluate basis functions which is automatically compiled and used in the Monte Carlo code, enabling larger simulations and improved convergence.
Most input and output files are stored in JavaScript Object Notation (JSON) file formats, which is widely used and highly readable.
Weak coupling between CASM and DFT codes, so that CASM can be adapted to work with various existing and future codes.
Interoperability

## Slide 16: CASM Components:
"casm" command line executable, with JSON input files
  C++11 for "core" (symmetry, crystallography, basis sets, Monte Carlo)
  Doxygen documentation
Python wrappers, visualization, analysis
  "casm" Python module for standard usage interfaces
  DFT software wrappers for VASP & SeqQuest
  "casm-learn" coefficient fitting integrates with scikit-learn, deap (genetic algorithms)
  Easy integration with VESTA for viewing configurations
  Interactive visualization
Python PBS & Slurm interface for cluster job submission:

## Slide 17: CASM Components:
Public version:
  Occupation DoF & grand canonical Monte Carlo calculations
  "beta" canonical Monte Carlo calculations enabling a large number of possible occupation constraints
  Variance-constrained Monte Carlo to be released very soon
  Available on github:
    https://github.com/prisms-center/CASMcode
  Demo project with pre-calculated DFT training data:
    https://github.com/prisms-center/CASMcode_demo

## Slide 18: Near Future (next 0-2 yrs):
Much of this is also completed in part or in full internally, and needs to be completed or polished in some way for the public code.
Kinetics:
  Enumeration of atomic hops and local configurations, NEB calculation, local cluster expansion of activation energy, KMC
Phonons:
  Enumerate configurations for force constant calculation, dynamical matrix calculation, free energy calculation in quasi-harmonic approximation
Strain polynomials:
  Generate symmetrized strain Hamiltonian, enumerate strained configurations, DFT calculation, fit Hamiltonian coefficients
Gamma-surface:
  Setup gamma-surface geometries and perform DFT calculations
Composition & configurational order parameter dependent free energies
  Specify ordered configurations, generate order parameter, perform variance-constrained Monte Carlo calculations and free energy integration
Machine learning tools for optimal design of Monte Carlo calculations
Integration with Materials Commons

## Slide 19
v0.2.1 Now Available!